SPECIFICATION TEMPLATE

ULTRALIGN Non-combustible Aluminium Cladding System

# SCOPE OF WORK

The scope of work includes the design, supply, fabrication and installation ULTRALIGN Non-combustible Aluminium Cladding System, complete with all necessary sub-structures, anchors, hardware and fittings to provide a total installation and cladding system from the structure out.

# MATERIAL AND FINISHES

Cladding Material:

Aluminium cladding material shall be supplied by Blue Chip Group Pty Ltd (Ph: 1300 945 123)

comprising of solid extruded pre-finished aluminium cladding panels which are minimum 6063-T5 series marine-grade aluminium alloy.

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

Colour Selection:

Refer to exterior finishes schedule.

(Select colour code/s from the Finishes tab at the below link)

http://www.bluechipgroup.net.au/facade-cladding-perth/extruded-aluminium-cladding-perth

Fire Properties:

# Manufactured by Blue Chip Group Pty Ltd; ULTRALIGN is a DTS Non-Combustible product in accordance with the BCA/NCC when tested to AS1530.1 and AS1530.3.

Timber-look Coating:

| ITEM | TEST STANDARD | UNIT | RESULT |
| --- | --- | --- | --- |
| Non-combustible | AS 1530.1 | CSIRO | Pass |
| Non-combustible (DTS) – NCC 2019 | NCC C1.9(e)(v) | CSIRO | Pass |
| Ignitability Index | AS 1530.3 | AWTA* | 8 |
| Spread of Flame Index | AS 1530.3 | AWTA* | 0 |
| Heat Evolved Index | AS 1530.3 | AWTA* | 0 |
| Smoke Developed Index | AS 1530.3 | AWTA* | 4 |
| Group Number | NCC 2019 C1.10 | Equivalence | <1 |

Standard Powdercoat Colours:

| ITEM | TEST STANDARD | UNIT | RESULT |
| --- | --- | --- | --- |
| Non-combustible | AS 1530.1 | CSIRO | Pass |
| Non-combustible (DTS) – NCC 2019 | NCC C1.9(e)(v) | CSIRO | Pass |
| Ignitability Index | AS 1530.3 | CSIRO* | 0 |
| Spread of Flame Index | AS 1530.3 | CSIRO* | 0 |
| Heat Evolved Index | AS 1530.3 | CSIRO* | 0 |
| Smoke Developed Index | AS 1530.3 | CSIRO* | 3 |
| Group Number | NCC 2019 C1.10 | Equivalence | <1 |

*Always check the AS 1530.3 certificate to ensure the finish was applied to the aluminium

prior to conducting the testing. Note that this does NOT apply to the AS 1530.1 testing.

Physical Properties:

| ITEM | TEST STANDARD | UNIT | RESULT |
| --- | --- | --- | --- |
| Alloy Grade / Temper | Actual | - | 6063 T5 |
| Material Density | Actual | Kg/m3 | 2,709 |
| Magnesium Content | Actual | % | 0.7 |
| Silicon Content | Actual | % | 0.4 |
| Thermal Expansion | Actual | mm/m/°C | 0.025 |

Fixings:

Fasteners, including concealed screws, nuts, bolts and other items required for connecting aluminium to aluminium or aluminium to steel shall be in accordance with AS 3566.2 and of a type to suit its application and exposure conditions.

Class 1/2:	Internal applications.

Class 3:	External applications, moderate industrial and marine applications.

Class 4:	Severe marine applications

All fixing anchors, brackets and similar attachments used in the erections, shall be of aluminium, non-magnetic stainless steel, zinc coated steel, or hot dip zinc galvanised steel.

Dissimilar Materials:

Where two surfaces of dissimilar material come into contact, such surfaces shall be separated with a layer of PVC or Polyethylene tape or powder-coat finish.

Warranty:

ULTRALIGN shall be covered by a manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations and installation details. The warranty is subject to the cladding system being fabricated and installed by a manufacturer trained and approved installer with a minimum 5 years’ experience.

# INSTALLATION

# General Guidelines:

The cladding system shall be installed by an approved cladding subcontractor with a demonstrated experience of at least 5 years in the fabrication and installation of pre-finished cladding systems. All work to be carried out in accordance with the ULTRALIGN manufacturer's recommendations and installation manuals. All component parts shall be installed level, true to line with uniform joints and reveals.

# Installation Details:

# The panels shall be fabricated and installed in accordance with the most recent version of the ULTRALIGN Installation Details which are available online at www.bluechipgroup.net.au or by emailing sales@bluechipgroup.net.au or by calling 1300 945 123. (Only PDF installation details are available online. For CAD/DWG installation details email or call as above).

Technical Manual:

# The panels shall be fabricated and installed in accordance with the most recent version of the ULTRALIGN Technical Manual which is available online at www.bluechipgroup.net.au or by emailing sales@bluechipgroup.net.au or by calling 1300 945 123.

Sarking (Delete if using SINIAT WD as below – recommended):

Shall be FIRESPAN deemed-to-satisfy non-combustible sarking tested by a NATA accredited laboratory to AS 1530.1. Install and tape in accordance with AS 4200.2 to all cladding areas.

Rigid Sheathing Board (Best practice in lieu of Sarking):

Shall be SINIAT WD 12.5mm deemed-to-satisfy non-combustible, vapour permeable material which assists in achieving a 60/60/60 FRL when installed as per manufacturer’s directions.

Sub-framing System:

The sub-framing system to be attached to the main structure in a manner to ensure all applied loadings to the cladding is transferred back to the main structure. Size and spacing of top hat members shall be determined according to applied loads and deflection limitations. Top-hat spacings shall be maximum 600mm to adequately support the cladding system.

Acceptable Sub-framing manufacturers are:

- STUDTEK Facade Framing, 1300 945 123, sales@bluechipgroup.net.au.

Standards:

STUDTEK Zincalume Facade Framing is cold-formed according to AS/NZS:4600 from Zincalume G300 steel which is continuous hot-dipped aluminium/zinc alloy-coated structural steel as per AS:1397.

Cladding Trims:

Shall be CLADTRIM colour-matched trim system supplied by Blue Chip Group Pty Ltd and installed as required to waterproof the façade in accordance with the manufacturer’s details.

Trim Sealant:

All junctions are to be filled and sealed with PROLASTIK silicone based non-stain sealant to manufacturer’s specifications immediately prior to installing the outside CLADTRIM profile.

Installation System Code:

UL-GR-CSF: Concealed Screw Fix – Groove Profile

UL-BV-CSF: Concealed Screw Fix – Bevel Profile

UL-SM-CSF: Concealed Screw Fix – Seam Profile

(PDF & DWG construction details available on request)

(Delete options not required)

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.