SPECIFICATION TEMPLATE

ULTRANAMEL Vitreous Enamel Panel

- SCOPE OF WORK

The scope of work includes the design, supply fabrication and installation of ULTRANAMEL cladding material, complete with all necessary sub-structures, anchors, hardware and fittings to provide a total installation.

- MATERIAL AND FINISHES

Cladding Material:

The cladding shall be ULTRANAMEL supplied by Blue Chip Group Pty Ltd (Ph: 08 9451 2344) comprising of a 1.5mm decarbonised steel face-skin bonded to a 12mm aluminium honeycomb supporting panel with 0.5mm backing sheet. The panels shall be finished with minimum 250um of baked vitreous enamel coating comprising of base coat and coloured top-coats.

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

Colour Selection:

Refer to exterior finishes schedule.

(Select colour code/s from the Finishes tab at the below link) http://www.bluechipgroup.net.au/facade-cladding-perth/vitreous-enamel-panel-perth

Material Properties:

| - TEST STANDARD | - DESCRIPTION | - RESULT |
| --- | --- | --- |
| - ASTM B117-07a | - Salt spray test | - No visual change |
| - ASTM C538-83: 2009 | - Colour retention | - No colour change |
| - ASTM: C481 | - Aging of sandwich constructions | - No visual change |
| - BS 1344.1 | - Resistance to thermal shock | - No visual flaking or crazing of enamel |
| - BS 1344.2: 1975 | - Resistance to Citric Acid at room temperature | - Class AA |
| - BS 1344.5: 1984 | - Resistance to hot detergent solutions used for washing textiles | - No visible cracking |
| - BS 14483.1: 2004 | - Resistance to chemical corrosion | - Class AA (both Sulphuric and Citric Acid) |
| - BS 14483.2: 2004 | - Resistance to chemical corrosion by boiling acids, neutral liquid and/or their vapours | - No visible cracking |
| - BS EN 10209: 1996, Annex D | - Adherence level of enamel | - Class 1 |
| - BS EN 14483.4: 2004 | - Resistance to hot sodium hydroxide | - Rate of mass loss = 1.37g/m2/hr |
| - BS EN ISO 15695: 2001 | - Scratch resistance | - Complies |
| - BS EN ISO 28722: 2011, Clause 5.3 | - Resistance to abrasion | - Total Mass loss = 0.021g |
| - BS EN ISO 28722: 2011, Clause 5.4 | - Impact resistance | - No damage |
| - BS1344.21: 1993 | - Resistance to Impact Pistol Test | - No cracking, powdering off, spalling or chipping at maximum force |
| - BS EN ISO 8289: 2011 | - Low voltage test | - 0 Defects |
| - BS1344.6: 1971 | - Resistance to Alkali | - No visible change |

Fire Properties:

| ULTRANAMEL |  |  |  |
| --- | --- | --- | --- |
| TEST STANDARD | RESULT |  |  |
| AS1530.1 | PASS (Deemed Non-combustible) |  |  |
| AS1530.3 | PASS | Ignitability Index | 0 |
|  | PASS | Heat Evolved | 0 |
|  | PASS | Spread of Flame | 0 |
|  | PASS | Smoke Developed | 0-1 |

Fixings:

Fasteners, including concealed screws, nuts, bolts and other items required for connecting aluminium to aluminium or aluminium to steel shall be in accordance with AS 3566.2 and of a type to suit its application and exposure conditions.

Class 1/2:	Internal applications.

Class 3:	External applications, moderate industrial and marine applications.

Class 4:	Severe marine applications

All fixing anchors, brackets and similar attachments used in the erections, shall be of aluminium, non-magnetic stainless steel, zinc coated steel, or hot dip zinc galvanised steel.

Dissimilar Materials:

Where two surfaces of dissimilar material come into contact, such surfaces shall be separated with a layer of PVC or Polyethylene tape or powder-coat finish.

Warranty:

ULTRANAMEL shall be covered by a manufacturer’s warranty for a minimum period of 10 years, the warranty is subject to being installed according to the installation manual by an approved ULTRANAMEL installer.

- INSTALLATION

The cladding system shall be installed by an approved cladding subcontractor with a demonstrated experience of at least 5 years in the fabrication and installation of pre-finished cladding systems. All work to be carried out in accordance with the ULTRANAMEL manufacturer's recommendations and installation manuals.

Sarking:

Shall be FIRESPAN deemed-to-satisfy non-combustible sarking tested by a NATA accredited laboratory to AS 1530.1. Install and tape in accordance with AS 4200.2 to all cladding areas.

Sub-framing System:

The sub-framing system to be attached to the main structure in a manner to ensure all applied loadings to the cladding is transferred back to the main structure. Size and spacing of top hat members shall be determined according to applied loads and deflection limitations. Top-hat spacings shall be maximum 600mm to adequately support the cladding system.

Acceptable Sub-framing manufacturers are:

- STUDTEK Facade Framing, 08 9451 2344, sales@bluechipgroup.net.au.

Standards

STUDTEK Zincalume Facade Framing is cold-formed according to AS/NZS:4600 from Zincalume G300 steel which is continuous hot-dipped aluminium/zinc alloy-coated structural steel as per AS:1397.

Panel Joint Sealant:

Panel joints to be filled and sealed with PROLASTIK silicone based non-stain sealant over open cell foam backing rod to manufacturer’s specifications.

Installation System Code:

UN-25-CCF: Concealed Cassette Fix (PDF & DWG construction details available on request)

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.