SPECIFICATION TEMPLATE

# FIRESPAN Non-combustible Sarking

# Sarking Material:

The sarking material shall be FIRESPAN deemed-to-satisfy non-combustible sarking in accordance with the latest version of the NCC and tested by a NATA accredited laboratory to AS 1530.1, AS 1530.2 and AS 1530.3 supplied by Blue Chip Group Pty Ltd (Ph: 1300 945 123).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

Fire Properties:

| ITEM | TEST STANDARD | LAB. | RESULT |
| --- | --- | --- | --- |
| Non-combustible as per C1.9(e)(vii) | AS 1530.1 | CSIRO | Pass |
| Flammability Index as per C1.9(e)(vi) | AS 1530.2 | AWTA | <5 |
| Ignitability Index | AS 1530.3 | AWTA | 0 |
| Spread of Flame Index | AS 1530.3 | AWTA | 0 |
| Heat Evolved Index | AS 1530.3 | AWTA | 0 |
| Smoke Developed Index | AS 1530.3 | AWTA | 0-1 |

# Physical Properties:

| ITEM | TEST STANDARD | UNIT | RESULT |
| --- | --- | --- | --- |
| Duty / Tensile Strength | AS 4200.1 | Classification | Extra Heavy |
| Edge Tear Resistance | AS 4200.1 | Classification | Extra Heavy |
| Dry Delamination | AS 4201.1 | - | Pass |
| Wet Delamination | AS 4201.2 | - | Pass |
| Shrinkage | AS 4201.3 | % | 0 |
| Water Barrier | AS 4201.4 | Silver White | Pass Pass |
| Emittance (silver foil facing) | AS 4201.5 AS 4201.5 | Value Reflectance | 0.05 95% |
| Water Absorbency | AS 4201.6 | Classification | Low |
| Vapour Transmission | ASTM E96 | g/h.m2 g/24h./m2 | 0.006 0.151 |
| Vapour Permeance | ASTM E96 | μg/N.s | 0.001 |
| Vapour Barrier | NCC 2019 (VCM) | Classification | Class 1 |
| Vapour Resistance | ASTM E96 | MN.s/g | 4483.6 |
| Burst Force | AS 2001.2.19 | N | 758 |
| Bursting Strength | AS 4200.1 | Classification | Light Wall |

# Installation:

# The FIRESPAN sarking shall be installed and taped as per AS 4200.2 in accordance with manufacturers recommendations to comply with all NCC and other statutory requirements.

Warranty:

FIRESPAN sarking shall be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.