SPECIFICATION TEMPLATE

# IBOARD Rigid Insulation Board – Concealed Brick Cavity, Soffit Applications & Frame Wall

# Insulation Material:

# The concealed cavity / soffit insulation / frame wall shall be IBOARD ____ mm thick, with a thermal value of R____, comprising a closed-cell CFC/HCFC-free, zero ozone depletion potential (ODP), non-corrosive, zero formaldehyde content, rigid thermoset polyisocyanurate foam core with two reflective gas-tight aluminium foil facings, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 1300 945 123).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

# Fire Performance:

# In accordance with NCC 2019 Specification C1.10, Table 4, IBOARD being a concealed insulation material, achieves the following results when tested to AS 1530.3:

# •	Ignitability Index:		0

# •	Spread of Flame Index:	0

# •	Heat Evolved Index:		0

# •	Smoke Developed Index:	2

# Physical Properties:

# •	Bulk Density:			± 32 kg/m3

# •	Compressive Strength:		≥150 kPa (15 ton/m² at 10% deformation)

# •	Closed Cells:			90-95% minimum

# •	Tensile Strength:		80 kPa

# Thermal Performance:

# •	Thermal Conductivity: 		ASTM C518: 0.022 W/mK

# •	Emittance of Foil Facings:	ASTM-E408-71: 0.05

Thickness & Material R-value:

| IBOARD (mm) | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material R-Value | 1.36 | 1.82 | 2.27 | 2.73 | 3.18 | 3.64 | 4.09 | 4.55 |

# Safety & Environmental:

# •	Formaldehyde Content:	0%

# •	CFC / HCFC Content:		0%

# •	Ozone Depletion:		0%

# •	Corrosive Content:		0%

# Installation:

# The IBOARD rigid insulation shall be installed as per manufacturers recommendations, concealed inside a brick cavity wall, inside a plasterboard lined frame wall or behind a suspended ceiling in under slab soffit applications to comply with NCC 2019 requirements. If exposed insulation is required use IBOARD G1 or IBOARD F17.

Warranty:

IBOARD insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.