SPECIFICATION TEMPLATE

# IBOARD P17 Insulated Plasterboard Lining – Exposed Internal Wall Lining Applications

# Insulation Material:

# The exposed insulated internal wall lining shall be IBOARD P17 ____ mm thick, with a thermal value of R ____, comprising a closed-cell CFC/HCFC-free, zero ozone depletion potential (ODP), non-corrosive, zero formaldehyde content, rigid thermoset polyisocyanurate foam core with a non-combustible 10mm plasterboard facer, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 08 9451 2344).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

# Fire Properties:

# In accordance with NCC 2019, IBOARD P17 exposed facer achieves the following results:

# •	NCC C1.9(e)(i):	DTS Non-combustible

# •	Group Rating:		1

# •	Spread-of-Flame:	0

# •	Smoke-Index:		3

# The IBOARD P17 rigid insulation shall be installed as per manufacturers recommendations direct to furring channels or stud frames to provide a Group 1 rated lining material to comply with NCC 2019 requirements. If the insulation is part of an external wall of a building required to be A or B construction, consider using IROCK non-combustible insulation material.

# Thermal Performance:

# Thermal Conductivity: 		ASTM C518: 0.022 W/mK (Insulation)

# Thermal Conductivity: 		ASTM C518: 0.170 W/mK (Facer)

# Safety and Environmental:

# Insulation shall be 100% non-corrosive and comprised of a closed-cell CFC/HCFC-free and zero ozone-depletion potential (ODP) rigid thermoset polyisocyanurate foam core, manufactured using raw materials containing zero trace levels of formaldehyde.

# Technical Details:

# •	Bulk density:		± 32 kg/m3

# •	Compressive strength:	≥ 150 kPa (15 ton/m² at 10% deformation)

# •	Closed cells:		90-95% minimum

# •	Vapour diffusion:	PIR foam: μ = 60. ALU lamination: μ > 100,000

Thickness & Material R-value:

| IBOARD G1(mm) | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material R-Value | 1.42 | 1.88 | 2.33 | 2.79 | 3.24 | 3.70 | 4.15 | 4.61 |

Warranty:

IBOARD P17 insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike, and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.