SPECIFICATION TEMPLATE

# IBOARD P17 Insulated Plasterboard Lining – Exposed Internal Wall Lining Applications

# Insulation Material:

# The exposed insulated internal wall lining shall be IBOARD P17 ____ mm thick, with a thermal value of R ____, comprising a closed-cell CFC/HCFC-free, zero ozone depletion potential (ODP), non-corrosive, zero formaldehyde content, rigid thermoset polyisocyanurate foam core with a non-combustible 10mm plasterboard facer, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 1300 945 123).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

# Fire Performance:

# In accordance with NCC 2019 Specification C1.10, the IBOARD P17 exposed plasterboard facer, being the wall or ceiling lining, achieves the following results:

# •	NCC 2019 Clause C1.9(e)(i):		DTS Non-combustible

# •	NCC 2019 C1.10 Group Rating:	1

# •	Smoke Growth Rate (SMOGRA):	<100

# •	Average Specific Extinction Area:	<250

# Physical Properties:

# •	Bulk density (Insulation):		± 32 kg/m3

# •	Compressive strength (Insulation):	≥150 kPa (15 ton/m² at 10% deformation)

# •	Closed cells (Insulation):		90-95% minimum

# •	Tensile Strength (Insulation):		80 kPa

# Thermal Performance:

# •	Thermal Conductivity (Insulation): 	ASTM C518: 0.022 W/mK

# •	Thermal Conductivity (Facer): 		ASTM C518: 0.170 W/mK

Thickness & Material R-value:

| IBOARD P17 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material R-Value | 1.42 | 1.88 | 2.33 | 2.79 | 3.24 | 3.70 | 4.15 | 4.61 |

# Safety & Environmental:

# •	Formaldehyde Content (Insulation):	0%

# •	CFC / HCFC Content (Insulation):	0%

# •	Ozone Depletion (Insulation):		0%

# •	Corrosive Content (Insulation):		0%

# Installation:

# The IBOARD P17 rigid insulation shall be installed as per manufacturers recommendations and in accordance with all relevant standards to provide a Group 1 rated lining material compliant with NCC 2019 requirements. If the insulation is part of an external wall of a building required to be A or B construction, consider using IROCK non-combustible insulation material.

Warranty:

IBOARD P17 insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike, and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.