SPECIFICATION TEMPLATE

# IBOARD G1 Group 1 Soffit Insulation Board – Exposed Under-slab Soffit Applications

# Insulation Material:

# The exposed under-slab soffit insulation shall be IBOARD G1 ____ mm thick, with a thermal value of R ____, comprising a closed-cell CFC/HCFC-free, zero ozone depletion potential (ODP), non-corrosive, zero formaldehyde content, rigid thermoset polyisocyanurate foam core with a non-combustible 6mm fibre cement facer, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 08 9451 2344).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

# Fire Properties:

# In accordance with NCC 2019, IBOARD G1 exposed facer achieves the following results:

# •	C1.9(e)(iv):		DTS Non-combustible

# •	Group Rating:		1

# •	Spread-of-Flame:	0

# •	Smoke-Index:		0-1

# The IBOARD G1 rigid insulation shall be installed as per manufacturers recommendations direct to underside of concrete slab to provide a Group 1 rated lining material in accordance with AS 5637 to comply with NCC 2019 requirements. If the insulation is proposed to be concealed behind a suspended ceiling, consider using standard IBOARD rigid insulation board.

# Thermal Performance:

# Thermal Conductivity: 		ASTM C518: 0.022 W/mK (Insulation)

# Thermal Conductivity: 		ASTM C518: 0.230 W/mK (Facer)

# Safety and Environmental:

# Insulation shall be 100% non-corrosive and comprised of a closed-cell CFC/HCFC-free and zero ozone-depletion potential (ODP) rigid thermoset polyisocyanurate foam core, manufactured using raw materials containing zero trace levels of formaldehyde.

# Technical Details:

# •	Bulk density:		± 32 kg/m3

# •	Compressive strength:	≥ 150 kPa (15 ton/m² at 10% deformation)

# •	Closed cells:		90-95% minimum

# •	Vapour diffusion:	PIR foam: μ = 60. ALU lamination: μ > 100,000

Thickness & Material R-value:

| IBOARD G1(mm) | 36 | 46 | 56 | 66 | 76 | 86 | 96 | 106 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material R-Value | 1.38 | 1.84 | 2.29 | 2.75 | 3.20 | 3.66 | 4.11 | 4.57 |

Warranty:

IBOARD G1 insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike, and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.