SPECIFICATION TEMPLATE

# IBOARD G1 Group 1 Insulated Soffit Lining – Exposed Under-slab Soffit Applications

# Insulation Material:

# The exposed under-slab soffit insulation shall be IBOARD G1 ____ mm thick, with a thermal value of R ____, comprising a closed-cell CFC/HCFC-free, zero ozone depletion potential (ODP), non-corrosive, zero formaldehyde content, rigid thermoset polyisocyanurate foam core with a non-combustible 6mm fibre cement facer, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 1300 945 123).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

# Fire Performance:

# In accordance with NCC 2019 Specification C1.10, the IBOARD G1 exposed fibre cement facer, being the wall or ceiling lining, achieves the following results:

# •	NCC 2019 Clause C1.9(e)(iv):		DTS Non-combustible

# •	NCC 2019 C1.10 Group Rating:	1

# •	Smoke Growth Rate (SMOGRA):	<100

# •	Average Specific Extinction Area:	<250

# Physical Properties:

# •	Bulk density (Insulation):		± 32 kg/m3

# •	Compressive strength (Insulation):	≥150 kPa (15 ton/m² at 10% deformation)

# •	Closed cells (Insulation):		90-95% minimum

# •	Tensile Strength (Insulation):		80 kPa

# Thermal Performance:

# •	Thermal Conductivity (Insulation): 	ASTM C518: 0.022 W/mK

# •	Thermal Conductivity (Facer): 		ASTM C518: 0.230 W/mK

Thickness & Material R-value:

| IBOARD G1 | 36 | 46 | 56 | 66 | 76 | 86 | 96 | 106 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material R-Value | 1.38 | 1.84 | 2.29 | 2.75 | 3.20 | 3.66 | 4.11 | 4.57 |

# Safety & Environmental:

# •	Formaldehyde Content (Insulation):	0%

# •	CFC / HCFC Content (Insulation):	0%

# •	Ozone Depletion (Insulation):		0%

# •	Corrosive Content (Insulation):		0%

# Installation:

# The IBOARD G1 rigid insulation shall be installed as per manufacturers recommendations and in accordance with all relevant standards to provide a Group 1 rated lining material compliant with NCC 2019 requirements. If the insulation is proposed to be concealed behind a suspended ceiling, consider using standard IBOARD rigid insulation board.

Warranty:

IBOARD G1 insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike, and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.