SPECIFICATION TEMPLATE

# IROCK Non-combustible Insulation – Concealed Brick Cavity, Soffit Applications & Frame Wall

# Insulation Material:

# The concealed cavity / soffit insulation / frame wall shall be IROCK ____ mm thick, with a thermal value of R____, manufactured by spinning a molten mixture of natural rock and other additives to create fine wool-like fibres which are bonded together using a thermoset resin to form a rigid non-combustible insulation board, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 1300 945 123).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

Fire Properties:

# Manufactured by Blue Chip Group Pty Ltd; IROCK is a DTS non-combustible product in accordance with the BCA/NCC when tested to AS1530.1 and AS1530.3.

| ITEM | TEST STANDARD | UNIT | RESULT |
| --- | --- | --- | --- |
| Non-combustible | AS 1530.1 | CSIRO | Pass |
| Ignitability Index | AS 1530.3 | AWTA | 0 |
| Spread of Flame Index | AS 1530.3 | AWTA | 0 |
| Heat Evolved Index | AS 1530.3 | AWTA | 0 |
| Smoke Developed Index | AS 1530.3 | AWTA | 0-1 |

# Physical Properties:

# •	Bulk Density:			±100kg/m3

# •	Compressive Strength:		≥10 KN/m2

# •	Service Temperature:		<750°C

# •	Melting Temperature:		<1000°C

# •	Rockwool Content:		>95%

# •	Resin Content	:		<5%

# •	Moisture Absorption:		<1.1%

# •

# Thermal Performance:

# •	Thermal Conductivity: 		ASTM C518: 0.036 W/mK

Thickness & Material R-value:

| IROCK (mm) | 40 | 60 | 80 | 100 |
| --- | --- | --- | --- | --- |
| Material R-Value | 1.11 | 1.67 | 2.22 | 2.78 |

# Installation:

# The IROCK rigid insulation shall be installed as per manufacturers recommendations, concealed inside a brick cavity wall, inside a plasterboard lined frame wall or to an exposed ceiling in under slab soffit applications to comply with NCC 2019 requirements. If a facer is required for aesthetic reasons in exposed applications, consider specifying IROCK PLUS with white prefinished facer.

Warranty:

IROCK insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.