SPECIFICATION TEMPLATE

# IROCK PLUS Non-Combustible Soffit Insulation – Exposed Under-slab Soffit Applications

# Insulation Material:

# The exposed under-slab soffit insulation shall be IROCK PLUS ____ mm thick, with a thermal value of R ____, comprising a non-combustible, prefinished, rigid mineral rock wool core with a non-combustible prefinished white facer, tested in accordance with AS/NZ standards to comply with the BCA/NCC and manufactured by Blue Chip Group Pty Ltd (Ph: 1300 945 123).

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

# Fire Performance:

# In accordance with NCC 2022 Clause C2D10, (previously NCC 2019 Clause C1.9) the IROCK PLUS non-combustible soffit insulation achieves the following fire performance results:

# •	NCC 2022 Clause C2D10(6)(g):	DTS Non-combustible

# •	Insulation Combustibility		AS 1530.1 Pass

# •	Facer Combustibility:			AS 1530.1 Pass

# •	Spread-of-Flame Index			AS 1530.3 = 0

# •	Smoke Developed Index		AS 1530.3 = 0-1

# Physical Properties:

# •	Bulk Density (Insulation):		100 kg/m3

# •	Compressive strength (Insulation):	10 Kn/m²

# Thermal & Acoustic Performance:

# •	Thermal Conductivity (Insulation): 	ASTM C518: 0.036 W/mK

# •	Acoustic Performance (Insulation):	ISO-354 2006: NRC 1.0

Thickness & Material R-value:

| IROCK PLUS | 60 | 80 | 100 | 120 |
| --- | --- | --- | --- | --- |
| Material R-Value | 1.67 | 2.22 | 2.78 | 3.33 |

# Other thickness available on request. MOQ and lead times will apply.

# Safety & Environmental:

# •	Rockwool Content:	>95

# •	Resin Content:		<5

# •	Water Absorption:	<1.1%

# •	Fungal Resistance:	Pass

# •	Core Corrosivity:	7-9

# Installation:

# The IROCK PLUS non-combustible soffit insulation shall be installed as per manufacturers recommendations and in accordance with all relevant standards to provide a non-combustible lining material compliant with NCC 2022 requirements.

Warranty:

IROCK PLUS insulation to be covered by manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike, and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.