SPECIFICATION TEMPLATE

CLADTRIM Colour-matched Cladding Trims

- SCOPE OF WORK

The scope of work includes the design, supply, fabrication and installation CLADTRIM Colour-matched Cladding Trims, complete with all necessary sub-structures, anchors, hardware and fittings to provide a total installation and weather-proof cladding system.

- MATERIAL AND FINISHES

Cladding Trims:

Shall be proprietary CLADTRIM Colour-matched Cladding Trims supplied by Blue Chip Group Pty Ltd (Ph: 08 9451 2344)

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

Colour Selection:

Refer to exterior finishes schedule.

(Select colour code/s from the Finishes tab at the below link) http://www.bluechipgroup.net.au/timber-cladding-perth/cladding-trims-perth

Fire Properties:

- Manufactured by Blue Chip Group Pty Ltd; CLADTRIM extrusions are DTS Non-Combustible product in accordance with the BCA/NCC when tested to AS1530.1 and AS1530.3.

| CLADTRIM |  |  |  |
| --- | --- | --- | --- |
| TEST STANDARD | RESULT |  |  |
| AS1530.1 | PASS (Deemed Non-combustible) |  |  |
| AS1530.3 | PASS | Ignitability Index | 8 |
|  | PASS | Heat Evolved | 0 |
|  | PASS | Spread of Flame | 0 |
|  | PASS | Smoke Developed | 4 |

*Always check the AS 1530.3 certificate to ensure the finish was applied to the aluminium

prior to conducting the testing. Note that this does NOT apply to the AS 1530.1 testing.

Applied Finish:

The external panel surface shall be factory prefinished by the manufacturer with commercial grade thermosetting ‘matt-effect’ powder-coat finish in the selected proprietary CLADTRIM timber-look coating.

Fixings:

Fasteners, including concealed screws, nuts, bolts and other items required for connecting aluminium to aluminium or aluminium to steel shall be in accordance with AS 3566.2 and of a type to suit its application and exposure conditions.

Class 1/2:	Internal applications.

Class 3:	External applications, moderate industrial and marine applications.

Class 4:	Severe marine applications

All fixing anchors, brackets and similar attachments used in the erections, shall be of aluminium, non-magnetic stainless steel, zinc coated steel, or hot dip zinc galvanised steel.

Dissimilar Materials:

Where two surfaces of dissimilar material come into contact, such surfaces shall be separated with a layer of PVC or Polyethylene tape or powder-coat finish.

Warranty:

CLADTRIM shall be covered by a manufacturer’s warranty for a minimum period of 10 years. All work to be carried out in accordance with the manufacturer's recommendations and installation details. The warranty is subject to the cladding system being fabricated and installed by a manufacturer trained and approved installer with a minimum 5 years’ experience.

- INSTALLATION

The cladding system shall be installed by an approved cladding subcontractor with a demonstrated experience of at least 5 years in the fabrication and installation of pre-finished cladding systems. All work to be carried out in accordance with the CLADTRIM manufacturer's recommendations and installation manuals. All component parts shall be installed level, true to line with uniform joints and reveals.

Sarking:

Shall be FIRESPAN deemed-to-satisfy non-combustible sarking tested by a NATA accredited laboratory to AS 1530.1. Install and tape in accordance with AS 4200.2 to all cladding areas.

Sub-framing System:

The sub-framing system to be attached to the main structure in a manner to ensure all applied loadings to the cladding is transferred back to the main structure. Size and spacing of top hat members shall be determined according to applied loads and deflection limitations. Top-hat spacings shall be maximum 600mm to adequately support the cladding system.

Acceptable Sub-framing manufacturers are:

- STUDTEK Facade Framing, 08 9451 2344, sales@bluechipgroup.net.au.

Standards:

STUDTEK Zincalume Facade Framing is cold-formed according to AS/NZS:4600 from Zincalume G300 steel which is continuous hot-dipped aluminium/zinc alloy-coated structural steel as per AS:1397.

Cladding Trims:

Shall be CLADTRIM colour-matched trim system supplied by Blue Chip Group Pty Ltd and installed as required to water-proof the façade in accordance with the manufacturer’s details.

Trim Sealant:

All junctions are to be filled and sealed with PROLASTIK silicone based non-stain sealant to manufacturer’s specifications immediately prior to installing the outside CLADTRIM profile.

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.