SPECIFICATION TEMPLATE

SELEKTA Timber Composite Cladding

- SCOPE OF WORK

The scope of work includes the design, supply, fabrication and installation SELEKTA Timber Composite Cladding, complete with all necessary sub-structures, anchors, hardware and fittings to provide a total installation and cladding system from the structure out.

- MATERIAL AND FINISHES

Cladding Material:

The cladding shall be SELEKTA Timber Composite Cladding supplied by Blue Chip Group Pty Ltd (Ph: 08 9451 2344) consisting of a particle wood core of processed timber exclusively from untreated pulpwood in the form of wood shavings, thinning material and round timber from sustainable, domestic forestry. Timber from tropical climates shall not be used. The binding agent used is a thermosetting artificial resin with building authority approval for outdoor use and as a wood preservative, we use an eco-friendly boron-based product with building authority approval that does not contain lindane or PCP. A mixture of boric acid and borax is used as a fire protection agent and no isocyanates, phosphates or halogens are added.

**NO ALTERNATIVE MATERIALS WILL BE ACCEPTED FOR THIS PROJECT**

Colour Selection:

Refer to exterior finishes schedule.

(Select colour code/s from the Finishes tab at the below link) http://www.bluechipgroup.net.au/timber-cladding-perth/timber-composite-cladding-perth.html

Fire Properties:

- Manufactured by Blue Chip Group Pty Ltd; SELEKTA Timber Composite Cladding is not non-combustible however it is compliant for type C construction and single dwelling residential projects up to Bushfire Attack Level BAL29. **For type A & B construction which now requires cladding to be non-combustible in accordance with NCC/BCA 2019, we recommend specifying ULTRAWOOD which is available in the same colours as SELEKTA. Click here for details**

| ULTRAWOOD |  |  |  |
| --- | --- | --- | --- |
| TEST STANDARD | RESULT |  |  |
| BAL Rating | Up to BAL29 |  |  |
| AS 3837 | Group Rating 3 |  |  |
| AS1530.3 | PASS | Ignitability Index | 13 |
|  | PASS | Heat Evolved | 0 |
|  | PASS | Spread of Flame | 4 |
|  | PASS | Smoke Developed | 3 |

Applied Finish:

Several layers of paper are impregnated with artificial resins for use as a coating, similar to high pressure exterior laminate. The surface and core are fused together without seams in a single process under the application of high pressure and heat. The surface is printed or dyed and a transparent weather resistant surface coating is applied on the decor side followed by coloured surface coating using a pure, water-based acrylate. The pigments added are free of toxic heavy metals (no lead, chrome or cadmium). The rear side is brown or milky white from the production process and offers no colour options.

Fixings:

Fasteners, including concealed screws, nuts, bolts and other items required for connecting aluminium to aluminium or aluminium to steel shall be in accordance with AS 3566.2 and of a type to suit its application and exposure conditions.

Class 1/2:	Internal applications.

Class 3:	External applications, moderate industrial and marine applications.

Class 4:	Severe marine applications

Dissimilar Materials:

Where two surfaces of dissimilar material come into contact, such surfaces shall be separated with a layer of PVC or Polyethylene tape or powder-coat finish.

Warranty:

SELEKTA shall be covered by a manufacturer’s warranty for a minimum period of 10 years.

- INSTALLATION

All work to be carried out in accordance with the SELEKTA manufacturer's recommendations and installation manuals. All component parts shall be installed level, true to line with uniform joints and reveals.

Sarking:

Shall be FIRESPAN deemed-to-satisfy non-combustible sarking tested by a NATA accredited laboratory to AS 1530.1. Install and tape in accordance with AS 4200.2 to all cladding areas.

Sub-framing System:

The sub-framing system to be attached to the main structure in a manner to ensure all applied loadings to the cladding is transferred back to the main structure. Size and spacing of top hat members shall be determined according to applied loads and deflection limitations. Top-hat spacings shall be maximum 600mm to adequately support the cladding system.

Acceptable Sub-framing manufacturers are:

- STUDTEK Facade Framing, 08 9451 2344, sales@bluechipgroup.net.au.

Standards:

STUDTEK Zincalume Facade Framing is cold-formed according to AS/NZS:4600 from Zincalume G300 steel which is continuous hot-dipped zinc alloy-coated structural steel as per AS:1397.

Cladding Trims:

Shall be CLADTRIM colour-matched trim system supplied by Blue Chip Group Pty Ltd and installed as required to water-proof the façade in accordance with the manufacturer’s details.

Trim Sealant:

All junctions are to be filled and sealed with PROLASTIK silicone based non-stain sealant to manufacturer’s specifications immediately prior to installing the outside CLADTRIM profile.

Installation System Code:

SK-GR-CSF: Concealed Screw Fix (PDF & DWG construction details available on request)

Disclaimer:

This Specification provided is generic in nature and is supplied in good faith for Specification guidance purposes only. It is understood that no 2 projects are alike and project specific information and advice should be obtained from necessary engineers, consultants and suppliers on a project to project basis.